Solution (The Experimental Question):

Task 1

1a.

((nominal=5´=0.08˚

| ((nominal (degree) | 0.08 |
| --- | --- |

1b.

If “a” is the distance between card and the grating and “r” is the distance between the hole and the light spot so we have

We want (0 to be zero i.e.

| ∆(0 | 0.4˚ |
| --- | --- |
| ( range of visible light (degree) | 13˚≤ ( ≤26˚ |

1c.

|  | (21.6±0.1) kΩ |
| --- | --- |
| ∆φ0 | 5´ = 0.08˚ |
|  | R=(192±1) kΩ |

∆φ0=5´ because

( = 5´ => R= (21.9±0.1) kΩ

( =-5´ => R= (21.9±0.1) kΩ

1d.

Table 1d. The measured parameters

| ( (degree) | Rglass(M() | (Rglass(M() | Rfilm(M() | (Rfilm(M() |
| --- | --- | --- | --- | --- |
| 15.00 | 3.77 | 0.03 | 183 | 3 |
| 15.50 | 2.58 | 0.02 | 132 | 2 |
| 16.00 | 1.88 | 0.01 | 87 | 1 |
| 16.50 | 1.19 | 0.01 | 51.5 | 0.5 |
| 17.00 | 0.89 | 0.01 | 33.4 | 0.3 |
| 17.50 | 0.68 | 0.01 | 19.4 | 0.1 |
| 18.00 | 0.486 | 0.005 | 10.4 | 0.1 |
| 18.50 | 0.365 | 0.005 | 5.40 | 0.03 |
| 19.00 | 0.274 | 0.003 | 2.66 | 0.02 |
| 19.50 | 0.225 | 0.002 | 1.42 | 0.01 |
| 20.00 | 0.200 | 0.002 | 0.880 | 0.005 |
| 20.50 | 0.227 | 0.002 | 0.822 | 0.005 |
| 21.00 | 0.368 | 0.003 | 1.123 | 0.007 |
| 21.50 | 0.600 | 0.005 | 1.61 | 0.01 |
| 22.00 | 0.775 | 0.005 | 1.85 | 0.01 |
| 22.50 | 0.83 | 0.01 | 1.87 | 0.01 |
| 23.00 | 0.88 | 0.01 | 1.93 | 0.02 |
| 23.50 | 1.01 | 0.01 | 2.14 | 0.02 |
| 24.00 | 1.21 | 0.01 | 2.58 | 0.02 |
| 24.50 | 1.54 | 0.01 | 3.27 | 0.02 |
| 25.00 | 1.91 | 0.01 | 4.13 | 0.02 |
| 16.25 | 1.38 | 0.01 | 66.5 | 0.5 |
| 16.75 | 1.00 | 0.01 | 40.0 | 0.3 |
| 17.25 | 0.72 | 0.01 | 23.4 | 0.2 |
| 17.75 | 0.535 | 0.005 | 12.8 | 0.1 |
| 18.25 | 0.391 | 0.003 | 6.83 | 0.05 |
| 18.75 | 0.293 | 0.003 | 3.46 | 0.02 |
| 19.25 | 0.235 | 0.003 | 1.76 | 0.01 |
| 19.75 | 0.195 | 0.002 | 0.988 | 0.005 |
| 20.25 | 0.201 | 0.002 | 0.776 | 0.005 |
| 20.75 | 0.273 | 0.003 | 0.89 | 0.01 |

| Range | Zero error |
| --- | --- |
| 200 MΩ | 0.9 MΩ |

1e.

In (=-20˚ => Rglass= (132± 2) kΩ  , Rfilm= (518±5) kΩ

| θ | Tfilm | θ | Tfilm |
| --- | --- | --- | --- |
| θ = -20˚ | 0.255 | 19.25 | 0.134 |
|  |  | 19.50 | 0.158 |
|  |  | 19.75 | 0.197 |
|  |  | 20.00 | 0.227 |
|  |  | 20.25 | 0.259 |
|  |  | 20.50 | 0.276 |
|  |  | 20.75 | 0.307 |

Graphics

We see that: T(( = 20.25˚) = T(( = -20˚)

| δ (degree) | 0.25±0.08 |
| --- | --- |

Task 2.

2a.

∆λ=2.9 cos(() (nm)

∆(αt)=

2b.

| (λ (nm) | 2.6-2.8 |
| --- | --- |

2c.

Table 2c. The calculated parameters using the measured parameters

| ( (degree) | λ (nm) | Ig/C(λ) (MΩ-1) | Is/C(λ) (MΩ-1) | Tfilm | αt | ((αt) |
| --- | --- | --- | --- | --- | --- | --- |
| 15.0 | 428 | 0.265 | 0.00546 | 0.0206 | 3.88 | 0.02 |
| 15.5 | 442 | 0.388 | 0.00758 | 0.0195 | 3.94 | 0.02 |
| 16.0 | 456 | 0.532 | 0.0115 | 0.0216 | 3.83 | 0.01 |
| 16.25 | 463 | 0.725 | 0.0150 | 0.0208 | 3.88 | 0.01 |
| 16.5 | 470 | 0.840 | 0.0194 | 0.0231 | 3.77 | 0.01 |
| 16.75 | 477 | 1.00 | 0.0250 | 0.0250 | 3.69 | 0.01 |
| 17.0 | 484 | 1.12 | 0.0299 | 0.0266 | 3.63 | 0.01 |
| 17.25 | 491 | 1.39 | 0.0427 | 0.0308 | 3.48 | 0.02 |
| 17.5 | 498 | 1.47 | 0.0515 | 0.0351 | 3.35 | 0.02 |
| 17.75 | 505 | 1.87 | 0.0781 | 0.0418 | 3.17 | 0.01 |
| 18.0 | 512 | 2.06 | 0.096 | 0.0467 | 3.06 | 0.01 |
| 18.25 | 518 | 2.56 | 0.146 | 0.0572 | 2.86 | 0.01 |
| 18.5 | 525 | 2.74 | 0.185 | 0.0676 | 2.69 | 0.01 |
| 18.75 | 532 | 3.41 | 0.289 | 0.0847 | 2.47 | 0.01 |
| 19.0 | 539 | 3.65 | 0.376 | 0.103 | 2.27 | 0.01 |
| 19.25 | 546 | 4.26 | 0.568 | 0.134 | 2.01 | 0.01 |
| 19.5 | 553 | 4.44 | 0.704 | 0.158 | 1.84 | 0.01 |
| 19.75 | 560 | 5.13 | 1.01 | 0.197 | 1.62 | 0.01 |
| 20.0 | 567 | 5.00 | 1.14 | 0.227 | 1.48 | 0.01 |
| 20.25 | 573 | 4.98 | 1.29 | 0.259 | 1.35 | 0.01 |
| 20.5 | 580 | 4.41 | 1.22 | 0.276 | 1.29 | 0.01 |
| 20.75 | 587 | 3.66 | 1.12 | 0.307 | 1.18 | 0.02 |
| 21.0 | 594 | 2.72 | 0.890 | 0.328 | 1.12 | 0.01 |
| 21.5 | 607 | 1.67 | 0.621 | 0.373 | 0.99 | 0.01 |
| 22.0 | 621 | 1.29 | 0.541 | 0.419 | 0.87 | 0.01 |
| 22.5 | 634 | 1.20 | 0.535 | 0.444 | 0.81 | 0.01 |
| 23.0 | 648 | 1.14 | 0.518 | 0.456 | 0.79 | 0.02 |
| 23.5 | 661 | 0.99 | 0.467 | 0.472 | 0.75 | 0.01 |
| 24.0 | 675 | 0.826 | 0.388 | 0.469 | 0.76 | 0.01 |
| 24.5 | 688 | 0.649 | 0.306 | 0.471 | 0.75 | 0.01 |
| 25.0 | 701 | 0.524 | 0.242 | 0.462 | 0.77 | 0.01 |

2d.

Graphics

| λmax(Iglass) | 564±5 (nm) |
| --- | --- |
| λmax(Ifilm) | 573±5 (nm) |

2e. Graphics

Task 3.

3a.

3b.

Table 3b. The calculated parameters for each measured data point

| ( (degree) | x (eV) | y ( eV2) | ∆x (eV) | ∆y (eV2) |
| --- | --- | --- | --- | --- |
| 15.00 | 2.898 | 126.6 | 0.019 | 2.0 |
| 15.50 | 2.806 | 121.9 | 0.018 | 1.9 |
| 16.00 | 2.720 | 108.8 | 0.017 | 1.5 |
| 16.25 | 2.679 | 107.8 | 0.016 | 1.4 |
| 16.50 | 2.639 | 98.9 | 0.016 | 1.3 |
| 16.75 | 2.600 | 92.0 | 0.015 | 1.2 |
| 17.00 | 2.563 | 86.3 | 0.015 | 1.2 |
| 17.25 | 2.527 | 77.4 | 0.014 | 1.1 |
| 17.50 | 2.491 | 69.7 | 0.014 | 1.0 |
| 17.75 | 2.457 | 60.9 | 0.013 | 0.8 |
| 18.00 | 2.424 | 55.1 | 0.013 | 0.8 |
| 18.25 | 2.392 | 46.8 | 0.013 | 0.6 |
| 18.50 | 2.360 | 40.4 | 0.012 | 0.6 |
| 18.75 | 2.330 | 33.1 | 0.012 | 0.5 |
| 19.00 | 2.300 | 27.3 | 0.012 | 0.4 |
| 19.25 | 2.271 | 20.91 | 0.011 | 0.36 |
| 19.50 | 2.243 | 17.07 | 0.011 | 0.27 |
| 19.75 | 2.215 | 12.92 | 0.011 | 0.22 |
| 20.00 | 2.188 | 10.51 | 0.010 | 0.19 |
| 20.25 | 2.162 | 8.53 | 0.010 | 0.17 |
| 20.50 | 2.137 | 7.56 | 0.010 | 0.14 |
| 20.75 | 2.112 | 6.23 | 0.010 | 0.18 |
| 21.00 | 2.088 | 5.43 | 0.009 | 0.11 |
| 21.50 | 2.041 | 4.06 | 0.009 | 0.09 |
| 22.00 | 1.997 | 3.02 | 0.009 | 0.06 |
| 22.50 | 1.954 | 2.52 | 0.008 | 0.08 |
| 23.00 | 1.914 | 2.26 | 0.008 | 0.09 |
| 23.50 | 1.875 | 1.98 | 0.008 | 0.07 |
| 24.00 | 1.838 | 1.94 | 0.007 | 0.06 |
| 24.50 | 1.803 | 1.84 | 0.007 | 0.05 |
| 25.00 | 1.769 | 1.86 | 0.007 | 0.04 |

3c.

Graphics

3d.

In linear range we have, m=213 (eV),  r2= 0.9986,  Eg=2.17 (eV)

and we have  so we find t= 206 (nm)

where δx & δy are the mean of error range of x & y

So

( ∆m ≈ 10 (eV) ( ∆t = t ( ∆m/(2 m)  ≈ 5 (nm)

Table 3d. The calculated values of Eg and t using Fig. 3

| Eg (eV) | (Eg (eV) | t (nm) | (t (nm) |
| --- | --- | --- | --- |
| 2.17 | 0.02 | 206 | 5 |

# Text boxes

Optical Axis

a

r

Reflected Beam

Incident Beam

Transmission

θ (degree)

Tfilm|θ=-20°

R-1 (MΩ-1)

Wavelength (nm)

glass

film

(α t h ν)2 (eV2)

hν (eV)